## SO-1000 /SO-5000

### Highly purified Silicone Oil for intraocular use

COMPOSITION 	1 ml contains highly pure silicone oil of 1000 / 5000 centistokes (Poly (dimethylsiloxane) (, designed for prolonged tamponade of the retina.

PHYSICAL PROPERTIES	Formula	(-Si (CH3)2O-(n(

Density	(g/cm3 at 24°C)	0.965

Refractive Index	(at 24°C)	1.405

Viscosity	(cs at 25°C)	1000 / 5000

INDICATIONS	Howard Instruments, Inc.-Silicone Oil 1000 / 5000 is used for intraocular tamponade in severe cases of retinal detachment, e.g. severe detachment with massive proliferative vitreo-retinopathy, traumatic detachment, giant tears as well as other retinal detachments, which cannot be treated with other forms of therapy.

CONTRAINDICATIONS	It is known that intraocular lenses made from silicone can be opacified by silicone oil. Therefore, 1000 /5000 should not be applied in eyes with silicone implants.

METHOD OF USAGE 	First the pouch has to be opened and the seal to be removed. The

AND DOSAGE	rubber needs to be cleaned with alcohol and the cap to be removed. It is suggested to pour into a sterile plastic syringe and to use a pneumatic or mechanical system to inject the oil into the eye. Due to the high viscosity of Howard Instruments, Inc. 1000 /5000 it is not suggested to inject the oil manually.

PRECAUTION OF USE	- Do not reuse

- Do not resterilize

- Do not use if the pouches are damaged

- Verify the expiration date

- Do not overfill the posterior segment with Howard Instruments, Inc. 1000 /5000

- Howard Instruments, Inc. oil1000 /5000 is free from preservatives.      Do not use for more than one patient

- Inject the product slowly, using a syringe driver

- If withdrawn, avoid leaving bubbles in the vitreo-retinal 	cavity

HOW SUPPLIED	SO-1000 /SO-5000 is available in vials of 10 ml

STERILIZATION	Heat sterilization with subsequent ETO sterilization (EN554)

STORAGE	At room temperature

SYMBOLS

Single use only			Sterile

See product description		Expiration date